## Slide 1
Nils Johan Engelsen, EPFL
Ultralow dissipation mechanical resonators for sensing and optomechanics

## Slide 2
LIGO scientific collaboration
Science 256, 325 (1992)
Rep. Prog. Phys. 72, 076901 (2009)
Image: Simulating Extreme Spacetimes Project

## Slide 3: Standard quantum limit for position measurements
Photon shot noise
Radiation pressure backaction
Sum
Standard quantum limit
V. B. Braginsky, J. Exp. Theor. Phys. (1968)
C. M. Caves, Phys. Rev. Lett. (1980)
A. A. Clerk et al., Rev. Mod. Phys. (2008)
Notes: We get half a zero-point motion each from shot noise and QBA and finally one zero-point motion contribution from the actual zpm of the resonator

## Slide 4: Quantum optomechanics

## Slide 5: Nanomechanical resonators
Sensors
Transducers
Quantum technologies

## Slide 6: Mechanical sensors
Magnetic resonance force microscopy
D. Rugar et al., Nature (2004)
M. Poggio and C. L. Degen, Nanotechnology (2010)
R. Fischer et al., New J. Phys. (2019)
U. Grob et al., Nano Lett. (2019)
Dark matter searches
Manley et al., Phys. Rev. Lett. (2021)
Carney et al., Quantum Sci. Technol. (2021)
Accelerometers
Krause et al., Nat. Photonics (2012)
Zhou et al., Optica (2021)
Image: F. Zhou, NIST
Mass sensors
Yang et al., Nano Lett. (2006)
Chaste et al., Nat. Nanotechnol. (2012)
Notes: Check if spin detection was published, maybe make images smaller and make more white space

## Slide 7: Mechanical transducers
Microwave-to-optical conversion
Higginbotham et al., Nat. Phys. (2017)
Forsch et al., Nat. Phys. (2020)
Jiang et al., Nat. Commun. (2020)
Arnold et al., Nat. Commun. (2020)
Optical RF detection
Bagci et al., Nature (2014)
A. Simonsen et al., Opt. Express (2019)
Two-mode entanglement
Barzanjeh et al., Nature (2020)
Chen et al., Nat. Commun. (2020)

## Slide 8: Mechanical resonators in quantum technologies
MacCabe et al., Science (2020)
Wallucks et al., Nat. Phys. (2020)
Coupling to superconducting qubits
Arrangoiz-Arriola et al.,
Nature (2019)
Chu et al., Science (2017)
Chu et al., Nature (2018)
Quantum memories
Chamberland et al., arXiv:2012.04108
Mechanical resonators are natural systems for encoding of cat state qubits
Teleportation
Fiaschi et al., Nat. Phot. (2021)
Notes: Mirhosseini et al., Nature (2020)

## Slide 9: Figures of merit for mechanical resonators
Thermal-limited force sensitivity
Thermal decoherence rate

## Slide 10: Smaller resonators limited by surface loss
Imboden et. al., Physics Reports (2014)
Villanueva and Schmid, Phys. Rev. Lett (2014)

## Slide 11: Dissipation dilution
González and Saulson,
J. Acoust. Soc. Am. (1994)
Gravitational potential
Optical trapping
Nanomechanical resonators
Ni et al., Phys. Rev. Lett. (2012)
Cripe et al., Nature (2019)
Unterreithmeier et. al. PRL (2010)
Yu et al., PRL (2012)

## Slide 12: A timeline of strained nanomechanics
Thompson et al.,
Nature (2008)
Millimeter-scale
membranes
Sankey et al.,
Phys. Rev. X (2016)
Trampoline
membranes
Soft-clamping
Y. Tsaturyan et. al.
Nat. Nano (2017)
Ghadimi et al.,
Science (2017)
Strain engineering
Higher aspect ratios and engineered geometry has enabled 100-1000 times higher mechanical quality factor

## Slide 13: Dissipation dilution: a toy model
Spring elongation
Hamiltonian
Tensioned spring system
Vibrational modes
S. A. Fedorov, PhD Thesis (2021)

## Slide 14: Dissipation dilution: introducing damping
A. S. Nowick and B. S. Berry, “Anelastic relaxation in crystalline solids” (1972)
V. B. Braginsky, V. P. Mitrofanov and V. I. Panov “Systems with Small Dissipation” (1985)
S. A. Fedorov, PhD Thesis (2021)
Voigt damper
Force
Quality factor

## Slide 15: Dissipation dilution in realistic structures
Fedorov, Engelsen et al. Phys. Rev. B (2019)

## Slide 16: Quality factor landscape
Material | Si3N4
Stress | 1.1 GPa
Thickness | 20 nm
Intrinsic Q | 2600

## Slide 17: Strained silicon-on-insulator material platform
TEM cross section
Dark-field electron holography
Potentially much higher intrinsic quality factor at low temperature

## Slide 18: Engineering dilution: soft clamping
Beccari et al., arXiv:2107.02124 (2021)
arXiv:2107.02124
Help | Advanced Search
Notes: Label mode shape

## Slide 19: Strained silicon nanobeams with Q~13 billion
Beccari et al., arXiv:2107.02124 (2021)

## Slide 20: Soft-clamped perimeter modes by vertex-clamping
Mechanical quality factors limited by torsion in the supports
Bereyhi et al., arXiv:2108.03615 (2021)

## Slide 21: Room temperature quality factor >3 billion
Bereyhi et al., arXiv:2108.03615 (2021)

## Slide 22: Coupled perimeter modes
Bereyhi et al., arXiv:2108.03615 (2021)

## Slide 23: Integrated optomechanical system
5 um
25 um
Room temperature ground state cooling
Force/spin sensing

## Slide 24: Devices with reflection pad

## Slide 25: Force sensing with mechanical resonators
Very sensitive to frequency fluctuations and alignment drift

## Slide 26: Feedback damping for broadened frequency response
Increase damping by viscous feedback:
Flatter frequency response without added noise
Spring constant
Damping rate
Measurement

## Slide 27: Attonewton force sensitivity at room temperature

## Slide 28: Applications in force microscopy
Hälg et al., Phys. Rev. Appl. (2021)
Tip+sample
Laser/optical cavity

## Slide 29: Dark matter searches
Figure from Carney et al., Quantum Sci. Technol. (2021)
Figure from Manley et al., Phys. Rev. Lett. (2021)
Particle-like dark matter: Search for impulses on detector
Ultralight dark matter: look for coherent force, mediated e.g. by B-L number

## Slide 30
M. Bereyhi
G. Huang
S. Fedorov
D. Visani
A. Beccari
A. Arabmoheghi
T. J. Kippenberg

## Slide 31: Strained silicon
For more information:
Strain engineering: Ghadimi et al., Science 360 (2018)
Dissipation dilution: S. A. Fedorov et al., Phys. Rev. B 99 (2019)
Binary tree beams: S. A. Fedorov, et al., Phys. Rev. Lett. 124 (2020)
Hierarchical resonators: Beccari et al., arXiv:2103.09785 (2021)
Strained silicon: Beccari et al., arXiv:2107.02124 (2021)
Perimeter modes: Bereyhi et al., arXiv:2108.03615 (2021)
Hierarchical structure
Strain engineering
Vertex clamping

## Slide 32: Backup slides

## Slide 33: Feedback cooling
Spring constant
Damping rate
Measurement
By applying a feedback force proportional to the velocity one can cool down the Brownian motion.
Langevin Stochastic force
Linear response (susceptibility)
Detection noise limits the performance of feedback stabilization.

## Slide 34: Soft clamping
Phononic crystal with defect localizes mechanical mode
Y. Tsaturyan et al., Nat. Nano. (2017)

## Slide 35: Record room temperature of 800 million at 1.3 MHz
Ghadimi et al., Science (2018)

## Slide 36: Quality factor landscape
Material | Si3N4
Stress | 1.1 GPa
Thickness | 20 nm
Intrinsic Q | 2600

## Slide 37: Soft clamping by hierarchical structure
Fedorov et al., Phys. Rev. Lett. (2020)
Wave derivative transformation

## Slide 38: Quality factor survey
Beccari et al., arXiv:2103.09785(2021)

## Slide 39: Quality factor of 800 million at 107 kHz
Beccari et al., arXiv:2103.09785(2021)
RT
6K
Force sensitivities surpassing the best AFM cantilevers

## Slide 40: Fractional spectral dimension
Fractal-like structures can have fractional spectral dimension:
Beccari et al., arXiv:2103.09785(2021)

## Slide 41: Hierarchical membranes
Trampoline resonators with at
Beccari et al., arXiv:2103.09785 (2021)
Topology optimization: Høj et al., arXiv:2103.15601 (2021)
Trampoline membranes:
Reinhardt et al., Phys. Rev. X (2016) Pluchar et al., Applied Optics (2020)
Norte et al., Phys. Rev. Lett. (2016)

## Slide 42: From toy model to realistic structures
For a deformation field, we have a strain tensor given by
Dissipation dilution requires:
Static strain
Geometric nonlinearity of strain
Especially strong for flexural (violin) modes
Fedorov, Engelsen et al. Phys. Rev. B (2019)

## Slide 43: From toy model to realistic structures
Fedorov, Engelsen et al. Phys. Rev. B (2019)
Unterreithmeier et. al. PRL 2010
Elastic energy
Bending energy
Lossless
Lossy

## Slide 44: Reduction of mode gradient over branches
Use divergence theorem combined with continuity of to obtain:
Balance of tension requires:
Giving:
Fedorov et al., Phys. Rev. Lett. (2020)

## Slide 45: Binary tree beam design
Cascaded branching of a nanobeam reduces the mode curvature at the boundaries
Useful parameters:
: Position on beam
: Total number of branches
: Length contraction ratio (), chosen to ensure the tree is not self-contacting
: Width ratio ()
: Angle between incoming and outgoing branch

## Slide 46: What limits the quality factor? Torsional motion
Out-of-plane motion of one branch induces torque on the next branch
Results in trade-off: reduction of bending at the boundaries vs. increased torsional energy

## Slide 47: Fractal beam design coefficients
Using the calculated mode shape we can evaluate the boundary energy, distributed bending energy, torsional energy and tensile energy to calculate and
Note: These are material independent
Boundary curvature
Distributed curvature
Torsional energy

## Slide 48: Si3N4 nanobeam process flow
Structures are patterned using
electron beam lithography
SiN
Si
FOX
Patterning
Upscaled version of the first lithography followed by deep reactive ion etching
SiN
Si
FOX
FOX
Gap definition
Si undercut using KOH
SiN
Si
Undercut

## Slide 49: Mechanical characterization setup
Resolves Brownian motion of mechanical modes
Ringdown measurements conducted by driving with PZT element
Homodyne phase is locked by changing frequency of second AOM drive

## Slide 50: Fabrication of sSi nanostrings
Patterning
Encapsulation
Undercut
Selective etch

## Slide 51: Temperature dependence of dissipation
Beccari et al., arXiv:2107.02124 (2021)
Notes: Observed some reversible degradation
Due to extra dissipation at clamping points, could be acoustic radiation or losses in the buried oxide layer at the pads

## Slide 52: Mechanical sensors
Gravitational astronomy
Force-detected magnetic resonance
Nature 430 329 (2004)
Nanotechnology 21, 342001 (2010)
LIGO scientific collaboration
Science 256, 325 (1992)
Rep. Prog. Phys. 72, 076901 (2009)
Image: Simulating Extreme Spacetimes Project
Force microscopy
Mass difference:
Tse et al., Phys. Rev. Lett. (2019)